## Slide 1: Tuning the ionic conductivity and electrochemical stability of Lithium through by the aliovalent substitution
Raul Artal López. July 2023

## Slide 2: Moving to Li metal
Current collector
Current collector
Main opportunities:
Higher theoretical energy densities (~400 Wh/kg)
Safety improvements due to the use of solid electrolytes
Main drawbacks of LIBs:
Lower energy density
Li dendrites evolution leading to short-circuit
Organic electrolytes
Safety issues
Ionic conductivity of solid-state electrolytes (SEs) (10-5 – 10-3 S/cm).
Huge resistances due to contact issues.
Interfacial processes during cycling.
Low cyclability.
Developing sustainable SEs avoiding the use of critical raw materials.

## Slide 3: Solid Electrolytes. Brief Overview
  Depending on the electrolyte used, solid state batteries are divided in two big families:
    Polymer-based ASSLiBs.
      Developed with polymeric materials as SEs.
      Thermal degradation issues limiting its applicability.
      Huge degradation on the Polymer/electrode interface.
      Low ionic conductivities (10-5 S/cm).
    Inorganic ASSLiBs.
      Developed with several different inorganic materials (oxides, halides, sulphides,…)
      Improvement in terms of safety
      Wide electrochemical stability window. (Better compatibility with high voltage cathodes)

## Slide 4: Solid Electrolytes. Brief Overview
  Depending on the electrolyte used, solid state batteries are divided in two big families:
    Polymer-based ASSLiBs.
      Developed with polymeric materials as SEs.
      Thermal degradation issues limiting its applicability.
      Huge degradation on the Polymer/electrode interface.
      Low ionic conductivities (10-5 S/cm)
J. Mater. Chem. A, 2016, 4, 10038-10069

## Slide 5: Solid Electrolytes. Brief Overview
  Depending on the electrolyte used, solid state batteries are divided in two big families:
    Polymer-based ASSLiBs.
      Developed with polymeric materials as SEs.
      Thermal degradation issues limiting its applicability.
      Huge degradation on the Polymer/electrode interface.
      Low ionic conductivities (10-5 S/cm).
    Inorganic ASSLiBs.
      Developed with several different inorganic materials (oxides, halides, sulphides,…)
      Improvement in terms of safety
      Wide electrochemical stability window. (Better compatibility with high voltage cathodes)

## Slide 6: Inorganic ASSLiBs
  Generally, inorganic solid electrolytes (ISEs) are considered as promising materials due to:
Promising ionic conductivities
Good Li+ diffusion
High thermal stability
Electronic insulators
Interface issues
Conductivity depends heavily on temperature
In contrast:

## Slide 7: Lithium Halides (Li3MX6)
  Since 2018, this family of compounds have gained so much attention since the preparation by Tetsuya Asano et. Al of Li3YCl6 and Li3YBr6 reporting ionic conductivities between 0.03 and 1.7·10-3 S/cm
    Wide electrochemical stability window (~4 V)
    Good chemical stability against typical cathodes as LCO (LiCoO2)
    Scalable and sustainable synthetic routes (i.e., aqueous based)
ACS Energy Lett., 2022, 7, 1776−1805

## Slide 8: Lithium Halides (Li3MX6)
  Since 2018, this family of compounds have gained so much attention since the preparation by Tetsuya Asano et. Al of Li3YCl6 and Li3YBr6 reporting ionic conductivities between 0.03 and 1.7·10-3 S/cm
    Wide electrochemical stability window (~4 V)
    Good chemical stability against typical cathodes as LCO (LiCoO2)
    Scalable and sustainable synthetic routes (i.e., aqueous based)
  Nevertheless, the ionic conductivities for these compounds are still low at low temperatures.
  Understanding the relationship between the structure and the ionic conductivity of these halides is essential.
ACS Energy Lett., 2022, 7, 1776−1805
Among the different families of halides, the most promising ones are the Li3MX6 since they show outstanding conductivities (~1 mS/cm), but there is still a lack of comprehension between the crystalline structure and the conductivity relationship

## Slide 9: Lithium Halides (Li3MX6)
  Then, how can we improve the ionic conductivity of these halides?
ACS Energy Lett., 2022, 7, 1776−1805
Central metal (M) substitution
Halide (X) substitution
Synthetic route selection

## Slide 10: Lithium Halides (Li3MX6)
  Then, how can we improve the ionic conductivity of these halides?
ACS Energy Lett. 2020, 5, 2, 533–539
Central metal (M) substitution
Halide (X) substitution
Synthetic route selection
X = 0 – 0.1  Trigonal pase (P-3m1) (Phase I)
X = 0.2  Orthorhombic (Pnma) (Phase II)
X = 0.367 – 0.6  “solid-solution region” (Phase III)
Li3-xEr1-xZrxCl6
Zr4+ (r = 72 pm); Er3+ (r = 89 pm)

## Slide 11: Lithium Halides (Li3MX6)
  Then, how can we improve the ionic conductivity of these halides?
J. Phys. Chem. C, 2023, 127, 1, 125–132
Central metal (M) substitution
Halide (X) substitution
Synthetic route selection
Li3YBrxCl6-x (x = 0-6)
0 < x < 1.5  Trigonal (P-3m1)
1.5 < x < 6  Monoclinic (C2/m)

## Slide 12: Lithium Halides (Li3MX6)
  Then, how can we improve the ionic conductivity of these halides?
Adv. Energy Mater. 2020, 10, 1903719
Central metal (M) substitution
Halide (X) substitution
Synthetic route selection
Li3ErCl6 (Mecanochemical vs. Thermochemical)
Local disorder induced by the synthetic route could tune the ionic conductivity of the electrolyte.

## Slide 13: Perspectives and work plan
FUNDAMENTAL
SYNTHESIS
APLICATION
Study and understanding of the influence of different crystal structures on ionic conductivity.
Processes and mechanisms of diffusion
Solid state NMR, EIS, XRD, NPD
Comprehensive synthesis and characterization of different halides of the families (Li3MX6 and Li2MX4).
Modulation of ionic conductivity by substitution and/or doping of the central metal (Al, Ca, Fe, Mn, Zr).
Thermochemical, mechanochemical, aqueous-based synthesis
Electrochemical characterization of the synthesized electrolytes (electrochemical stability window, galvanostatic cycling, ageing tests), both in half-cell and full cell configurations.
Compatibility study with different cathodes and interphase dissemination
Integration on large area battery devices by means of robot-casting printing technique

## Slide 14: Early Results
  Li3InCl6 solution-based synthesis
    LiCl + InCl3 stoichiometric mixture
    Dissolve in H2O (1:5 w/w) overnight at room temperature
    Heat at 60 ºC (333 K) until complete evaporation
    Drying at 180 ºC in vacuum for 18 h
Ea = 0.31 eV
(25 ºC) = 1 mS/cm
Monoclinic - C2/m (#12)

## Slide 15: Early Results
  Li2+xZr1-xFexCl6 aliovalent substitution of Zr(IV)
    LiCl + ZrCl4 + FeCl3 stoichiometric mixtures (2+x:1-x:x)
    Hand ground the metallic precursors
    Put the mixture in a 45 mL ZrO2 milling jar with ZrO2 of 5 mm diameter as grinding media
    All the preparation was done in an Ar filled Glovebox
σ(25 ºC) = 1 mS/cm
σ(25 ºC) = 0.4 mS/cm

## Slide 16: Conclusions
Li3InCl6 has been synthetized and the obtained conductivity values match those from the literature.
Iron (III) aliovalent substitution of Zr (IV) has shown to be beneficial at least in terms of ionic conductivity, however, more characterization is needed in order to fully understand the system.
This leaves the path opened to the development of new sustainable SEs based on non-critical raw materials such as Ca, Mg, Al, Fe, among others.

## Slide 17: Acknowledges
Dr. Ainara Aguadero and Dr. Ricardo Jiménez for the supervision of this thesis.
SEATBELT EU project. Funding
Energy Conversion, Harvesting and Storage group.
Dr. Fátima Esteban. X-ray Diffraction Unit, ICMM.

## Slide 18: Tuning the ionic conductivity and electrochemical stability of Lithium through by the aliovalent substitution
Raul Artal López. July 2023